Product / Process Change Notice

- Parts Affected:

- Chip process CP319, NPN silicon power transistors, wafers, and bare die.

- Extent of Change:

The CP319 wafer process has been discontinued and replaced with the CP212 wafer process. See figures 1 and 2 for details.

- Reason for Change:

New wafer process provides an improved and consistent yield. Revision 1 of this PCN was released to include additional “Part Numbers Affected” on the following page that were not included in the initial PCN release.

- Effect of Change:

The wafer process meets all electrical specifications of the individual devices listed on the following page.

- Effective Date of Change:

January 11, 2016

- Sample Availability:

- Please contact Salesperson or Manufacturer’s Representative.

- Qualification Tests:

| Test | Condition | Failure rate |
| --- | --- | --- |
| Resistance to Solder Shock | T =260⁰C ±5⁰C Dwell time = 10 sec. JESD22-B106 | 0/77 |
| High Temperature Storage Life/ bake test. | Specified temperature (-0/+10)°C, 1000 hours. JESD22-A103 | 0/77 |
| Temperature Cycling | T= -65⁰C to +150⁰C 1000 cycles. Dwell time = 15 min. JESD22-A104 | 0/77 |
| High Temperature Reverse Bias (HTRB) | T=125⁰C, t=48 hours, 80% MAX rated VCB JESD22-A108 | 0/77 |
| Highly Accelerated Temperature and Humidity Stress Test (HAST) | T = 130°C, RH = 85%, P = 33.3 psia, and t = 96 hours. Bias conditions per device specification sheet. JESD22-A110 | 0/77 |
| Accelerated Moisture Resistance Unbiased Autoclave | Temperature = 121⁰C ± 2⁰C; relative humidity = 100%; vapor pressure = 205kPa, 29.7 psia. t=48 hours JESD22-A102 | 0/77 |

- Figures:

Figure 1: CP319 Chip Geometry (Discontinued)		Figure 2: CP212 Chip Geometry

Wafer Diameter:		4 inch

Die Size:		87 x 87 mils

Die Thickness:		9.0 mils

Bond Pad Size (Emitter):	38 x 16 mils

Bond Pad Size (Base):	24 x 15 mils

Topside Metal:		Al (30,000Å)

Backside Metal:		Ti/Ni/Ag (11,000Å)

Wafer Diameter:		4 inch

Die Size:		80 x 99 mils

Die Thickness:		12 mils

Bond Pad Size (Emitter):	48 x 13 mils

Bond Pad Size (Base):	32 x 12 mils

Topside Metal:		Al (30,000Å)

Backside Metal:		Cr/Ni/Ag (16,000Å)

Part Numbers Affected:

- As per JEDEC standard JESD46, Customer Notification of Product/Process Changes by Solid-State Suppliers, a lack of acknowledgement of a PCN within thirty (30) days constitutes acceptance of the change.

- The undersigned acknowledges and accepts Central Semiconductor’s Product/Process Change Notification (PCN).

| - Company Name: |  |
| --- | --- |
| - Address: |  |
| - Printed Name: |  |
| - Title: |  |
| - Signature: |  |
| - Date: |  |