**Product / Process Change Notice**

**Parts Affected:**

Fast, hyperfast, superfast and ultrafast recovery rectifiers manufactured in DO-41, DPAK, D2PAK, SMA, SMAFL, SMB, SMC and SOD-123FL cases.

**Extent of Change:**

Additional wafer fab site.

**Reason for Change:**

As part of Central Semiconductor’s supply chain risk mitigation initiative, in an effort to ensure an undisrupted supply of product, an additional wafer fabrication site is being added for the referenced product families. Product specifications, quality and reliability are not impacted by this addition.

**Effect of Change:**

This addition does not affect the fit, form or function of the devices.

**Qualification:**

|  |  |  |  |
| --- | --- | --- | --- |
| **Test** | **Condition** | **Duration** | **Failure rate** |
| **Temperature Cycling (T.C.)** | TA= -55+0℃/-10℃ 10min(Min)  TA= +150+15℃/-0℃ 10min(Min)  Transfer time less than 1min.  The load should reach temp. within 15min | 1000 Cycles | 0/77  3 Lots |
| **High Temp. Storage Life (H.T.S.L.)** | TA= +150℃ | 1000 Hours | 0/77  3 Lots |
| **Continue Forward Operating Life (C.F.O.L)** | TA=+25℃, VR=100%VB  I=IO±10% DC supply | 168 Hours | 0/77  3 Lots |
| **Resistance to Solder Heat (R.S.H.)** | T =260°C ±5°C Dwell time = 10 sec. | 1 Cycle | 0/30  3 Lots |
| **Intermittent**  **Forward**  **Operation Life (I.O.L.)** | I=1.0 × IF DC supply  On time: 2mins at least,  Off time: 2mins at least | 15,000 Cycles | 0/77  3 Lots |
| **High Temp. Reverse Bias (H.T.R.B.)** | TA=+140℃, VR=80%VB  DC Supply | 96 Hours | 0/77  3 Lots |
| **Thermal Shock Test (T.S.T.)** | TA=0℃ (5 min) ~ +100℃ (5 min) | 100 Cycles | 0/77  3 Lots |

**Effective Date of Change:**

Existing inventory will be shipped until depleted.

**Sample Availability:**

Please contact your salesperson or manufacturer’s representative for samples.

**Part Numbers Affected:**

DO-41 case

DPAK case

D2PAK case

SMA case

SMAFL case

SMB case

SMC case

SOD-123FL case

CR1S-040

CUD3-02

CUDD8-04

CEN1253

CMR1H-04MFL

CMR1S-01

CMR3S-01

CMMR1F-02

CUD6-02C

CMR1S-02

CMR3S-02

CMMR1F-04

CMR2S-02

CMR3S-04

CMMR1F-06

CMR2S-04

CMR3S-06

CMMR1F-08

CMR2S-06

CMMR1S-02

CMMR1U-02

CMMR1U-04

CMMR1U-06

CMMR1U-08

As per JEDEC standard JESD46, Customer Notification of Product/Process Changes by Solid-State Suppliers, a lack of acknowledgement of a PCN within thirty (30) days constitutes acceptance of the change.

The undersigned acknowledges and accepts Central Semiconductor’s Product/Process Change Notification (PCN).

|  |  |
| --- | --- |
| Company Name: |  |
| Address: |  |
|  |
|  |
| Printed Name: |  |
| Title: |  |
| Signature: |  |
| Date: |  |